## Slide 1: Sustainable Manufacturing Case Study: Atomic Layer Deposition (ALD) Nano-Manufacturing Technology
Chris Yuan, Ph.D.
Department of Mechanical Engineering
University of Wisconsin-Milwaukee

## Slide 2
Introduction
Sustainability challenges of ALD
Case study: ALD of Al2O3
ALD theory
Overview
Design of ALD process for sustainability
Summary

## Slide 3
Introduction
Nano-manufacturing technology
Nano-manufacturing is the process of manipulation of matters in nano scale (between 1 and 100 nanometers) to develop nanomaterials, or fabricate 2D and 3D nanoscale structures.
Highly interdisciplinary: engineering, surface science, organic chemistry, molecular biology, semiconductor physics, micro-fabrication, etc.;
Versatile: microelectronics, energy, environmental and human health, etc..
J. Nanopart. Res., 15 (2013)
Chem. Vap. Deposition, 9 (2003) 327-332

## Slide 4
Introduction
Nano-manufacturing technology
Two main categories: top-down and bottom-up.
Top-down (Subtractive) techniques: methods, achieve nanoscale features through carving or grinding methods (e.g., lithography, etching, and milling).
Bottom-up(Additive) methods: form the nano structures through nucleation or growth from gas, liquid, or solid precursors by chemical or physical processes.
Journal of Industrial Ecology, 12 (2008) 329-359
Top-down techniques | Bottom-up techniques
Lithography | Vapor-phase techniques
Conventional lithography | Deposition techniques
Photolithography | Vapor phase epitaxy
E-beam lithography (for mask generation only) | Metal organic chemical vapor deposition
Next-generation lithography | Molecular beam epitaxy
Immersion lithography | Plasma-enhanced chemical vapor deposition
Lithography with lower wavelengths | Atomic layer deposition
than photolithography | Pulsed laser deposition
Extreme ultraviolet (soft X-ray) lithography | Sputtering
X-ray lithography | Evaporation
Lithography with particles | Nanoparticle/nanostructured materials
E-beam lithography | synthesis techniques
Focused ion-beam lithography | Evaporation
Nanoimprint lithography | Laser ablation
Step-and-flash imprint lithography | Flame synthesis
Soft lithography | Arc discharge
Etching | Liquid-phase techniques
Wet etching | Precipitation
Dry etching | Sol-gel
Reactive ion etching | Solvothermal synthesis
Plasma etching | Sonochemical synthesis
Sputtering | Microwave irradiation
 | Reverse micelle
Electrospinning | Electrodeposition
Milling | Self-assembly techniques
Mechanical milling | Electrostatic self-assembly
Cryomilling | Self assembled monolayers (SAMs)
Mechanochemical bonding | Langmuir-Blodgett formation
Major nano-manufacturing techniques

## Slide 5
Introduction
Atomic layer deposition (ALD)
Animation: ALD process.
Courtesy of Cambridge Nanotech
A vapor-phase additive thin film fabrication technique;
Operated by alternately injecting two or more chemical precursors into a chamber to enable sequential saturated surface reactions on substrates;

## Slide 6
Introduction
ALD cycle
ALD AB cycle
A typical ALD cycle involves two pulse steps and two purge steps;
Two precursors, one carrier gas (e.g., nitrogen, argon);
Pulse in milliseconds;
Purge in seconds.

## Slide 7
Introduction
ALD system
A typical thermal single-wafer ALD reactor mainly consists of a precursor delivery unit, a carrier gas delivery unit, a heating unit, a pumping unit and a chamber.
Courtesy of Cambridge Nanotech
Cambridge Nanotech S100 ALD system
Nanotech Savannah S100 ALD system

## Slide 8
Introduction
ALD types
Semicond. Sci. Technol., 27 (2012) 074002
Based on scalability and the process conditions
Based on scalability | Based on process conditions
Single-wafer ALD | Thermal ALD
Multi-wafer batch ALD | Plasma-enhanced ALD
Spatial ALD | Low temperature ALD
Roll-to-roll ALD | Low-pressure ALD
- | Atmospheric pressure ALD

## Slide 9
Introduction
ALD reactors
Semicond. Sci. Technol., 27 (2012) 074002
(a) Showerhead type single-wafer ALD reactor;
(b) Multi-wafer batch ALD reactor;
(c) In-line spatial ALD reactor;
(d) Roll-to-roll ALD reactor.

## Slide 10
Introduction
ALD advantages
Chem. Rev., 110 (2010) 111-131
Excellent uniformity of deposition;
Accurately-controlled film thickness;
Wide range of film materials.

## Slide 11
Introduction
ALD applications
Microelectronics
Energy conversion and storage
Medical and environmental health
Intel Corporation: Al2O3 high-k gate dielectric for its 45 nm CMOS.
IEEE International, 2007, pp. 247-250
Nanotechnology, 26 (2015) 064001
Surface sensitization
for solar cells
Int. Mater. Rev., 58 (2013) 113-129
Platinum coated on 20 nm pore size nanoporous alumina membranes

## Slide 12
Sustainability challenges
Sustainability challenges of ALD
Toxic chemical wastes and emissions
Toxic chemicals used as precursors;
Large amount of precursors end up with wastes;
The byproducts usually are major greenhouse gases.
Nano-wastes and nano-particle emissions
Nano-particles can be formed in ALD process;
Pose serious environmental and health issues.
High energy consumptions
ALD is an energy-intensive process;
Environmental problems associated with the high energy consumption, such as pollutants including CO2, CO, NOx, SOx from usage of fossil fuels.

## Slide 13
ALD theory
ALD process decoupling
Laminar flow (Momentum transport)
Heating (Convective heat transfer)
Species transport (Mass transfer)
Chemical reactions (Surface reactions)
Physical and chemical processes in ALD

## Slide 14
ALD theory
ALD process governing equations
1. Continuity Equation:
2. Momentum Transport within Laminar Flow:
3. Species Transport:
4. Energy Equation:
5. Surface Reaction: the rth irreversible surface reaction
where G, B, and S denote gaseous species, bulk (solid) species, and surface species in the
ALD chamber, respectively.
Reaction rate of the surface reaction:

## Slide 15
Enthalpy
E=Internal Energy
T=Temperature
p=Pressure
V=Volume
Q=Heat Transfer W=Work
Cp=Heat Capacity (constant pressure)
Enthalpy: H = E + pV
Specific Enthalpy: h = e + pv
1st Law of Thermodynamics: E2 - E1 = Q - W
For a constant pressure process: W = p(V2 - V1)
Q = Cp (T2 - T1)
(E2 + pV2) – (E1 + pV1) = Cp (T2-T1)
Then,
Definition of enthalpy:
H2 – H1 = Cp (T2 - T1)
h2 – h1 = cp (T2 - T1)
Specific Enthalpy:
ALD theory
Energy flow analysis

## Slide 16
Exergy
Exergy is the maximum useful work that could be obtained from the system
at a given state in specified environment.
The wasted work potential during a process as a result of irreversibilities.
Exergy Loss (Exergy destruction)
System State
Reference State
Exergy=Maximum work attainable by returning the system from the System State to the Reference State
System State
Reference State
Exergy=Minimum work needed to take the system from the Reference State to the System State
Exergy (B)
reference temperature (T0): 298.15K
reference pressure (p0): 1atm
Exergy Efficiency
ALD theory
Energy flow analysis

## Slide 17
Bin
(1-T0/T)Qin
Win
Bout
(1-T0/T)Qout
Wout
Physical exergy:
Chemical exergy:
Bph
Bch
Exergy
(B)
Exergy accompanying mass flow
Exergy accompanying work flow
Exergy accompanying heat flow
ALD theory
Energy flow analysis

## Slide 18
Deposition of Al2O3
The parameters of temperature and purge time are typical.
GPC is defined as growth per cycle.
Chemical Kinetics
Surface Chemistry
vs.
Experimental characterizations
ALD theory

## Slide 19
Measurement of nanoparticles
UCPC
UCPC measures concentration of nanoparticles.
SMPS is made up of combing electrostatic classifier and UCPC together.
It measures size distribution of nanoparticles
UCPC
Electrostatic Classifier
DMA
ALD theory

## Slide 20
Measurement of nanoparticles
Collection of nanoparticles
Charge nanoparticles using DMA.
When charged nanoparticles flow through the sampler with voltage, they will be collected on substrate.
DMA
Aerosol Sampler
ALD theory

## Slide 21
Case study: ALD of Al2O3
ALD of Al2O3
ALD of Al2O3 is studied as a model ALD process due to its high dielectric constant(k), high thermal stability and good adhesion to many surfaces.
Al2O3 thin film applications:
High-k gate dielectric in silicon microelectronics; dynamic random access memory (DRAM) with trench structures; etc.
IEEE International, 2007, pp. 247-250
TEM of high-k dielectric with metal gate for 45 nm PMOS transistor
300 nm Al2O3 ALD thin film on a Si wafer with a trench structure for DRAM application
Chem. Rev., 110 (2010) 111-131

## Slide 22
Most studied precursors:
Tri-methyl-aluminum [Al(CH3)3, or Al(Me)3, or TMA] as the metal provider; H2O as the oxidant.
The overall reaction with the two reactants:
In ALD, the reaction is separated into two half surface reactions:
Precursors for Al2O3 ALD
Case study: ALD of Al2O3
Metal provider | Oxidant
AlCl3 | H2O
AlCl3 | O2
AlBr3 | H2O
Al(CH3)3 | H2O
Al(CH3)3 | H2O2
Al(CH3)3 | O3
Al(CH3)3 | N2O
Al(CH3)3 | NO2
Al(CH3)3 | N2O4
ALD of Al2O3

## Slide 23
Modeling the ALD process
Numerical implementation
(a) Cambridge Nanotech Savannah S100 ALD system; (b) 3D model of the S100 ALD reactor system; (c) Fluid numerical domain based on S100 ALD reactor system.
Experimental results
Experimental investigation on the effects of purging time and process temperature: Al2O3 film growth rates in Å/cycle for: (a) 8s purging time; (b) 20s purging time.
Case study: ALD of Al2O3

## Slide 24
Fluid dynamics modeling
Precursor distributions during the full cycle of flow simulations for carrier gas flow rate: (a), (c) 20 sccm; (b), (d) 200 sccm;.
Precursor distribution contour plots for 20sccm flow rate: (a) TMA when purging ends; (b) Water when purging ends.
FIG.1. (a) Cambridge Nanotech Savannah S100 ALD system; (b) 3D model of the S100 ALD reactor system; (c) Fluid numerical domain based on S100 ALD reactor system.
(a)
(b)
Case study: ALD of Al2O3

## Slide 25
Water pulse
TMA pulse
The transient ALD process
Reactive deposition process
Case study: ALD of Al2O3

## Slide 26
ALD emission inventory
Two types of emissions: gases and nanoparticles
Gases
Gases are analyzed by Residual Gas Analyzer.
Greenhouse gaseous emissions, e.g., CH4.
Precursor wastes.
Nanoparticles
Nanoparticles collected by Aerosol Sampler;
Size measured by Scanning Mobility Particle Sizer Spectrometer (SMPS);
Concentration measured by Ultrafine Condensation Particle Counter (UCPC);
Composition analyzed by Energy-dispersive X-ray spectroscopy (EDS);
Nanoparticles characterized by Scanning Electron Microscope (SEM), Transmission Electron Microscopy (TEM).
Case study: ALD of Al2O3

## Slide 27
Measurement of gas emissions
A RGA is a small quadrupole mass spectrometer to measure gaseous components.
It is applied in high vacuum, usually around 1×10-7 torr.
Pressure of ALD system is much higher, so the measurements use capillary to inject sample and reduce pressure.
An example of result measured by RGA.
N2
CH4
H2O
Case study: ALD of Al2O3

## Slide 28
Emission of CH4 during 120 cycles of ALD reactions (25 ºC, 1 atm).
Measurement of gas emissions
An example of average concentration of gaseous emissions.
Component | Conc. (Vol. %)
N2 | 95.04
CH4 | 3.10
H2O | 1.86
Case study: ALD of Al2O3

## Slide 29
Emission of nanoparticles in 25 cycles of reactions
Measurement of nanoparticles
Case study: ALD of Al2O3

## Slide 30
Element | atom. %
C | 3.37 ± 1.07
Al | 4.40 ± 1.00
O | 3.86 ± 0.74
Cu* | 83.46 ± 16.11
F** | 4.96 ± 0.96
Element Components of Nano-particles
*Cu comes from the background signal of TEM grids.
** F is generated by pump.
Case study: ALD of Al2O3
Measurement of nanoparticles
Size distribution of nanoparticles.
TEM
SEM

## Slide 31
10 Pieces of Si wafer were installed along the pipeline.
The Si wafers were pretreated with HF (5%) and Piranha solution to remove SiO2 and carbon-containing chemicals on the surface.
The 10 pieces have the same time of reaction.
EDS measurements of deposition along the ALD system
# | C (atom. %) | Al (atom. %) | O (atom. %)
1 | 0.26±0.27 | 1.45±0.10 | 3.39±0.50
2 | 0.54±0.30 | 1.14±0.10 | 2.58±0.40
3 | 1.38±0.40 | 1.42±0.10 | 4.41±0.60
4 | 0.67±0.30 | 1.36±0.10 | 3.82±0.50
5 | 0.71±0.37 | 1.26±0.10 | 3.34±0.50
6 | 0.55±0.30 | 1.39±0.10 | 3.29±0.50
7 | 0.48±0.30 | 1.28±0.10 | 3.24±0.50
8 | 0.27±0.30 | 1.47±0.10 | 3.55±0.50
9 | 5.01±0.70 | 2.41±0.20 | 13.23±0.70
10 | 0.16±0.30 | 0.17±0.10 | 0.95±0.20
Case study: ALD of Al2O3
Nanoparticle distribution along pipeline

## Slide 32
Energy flow diagram of 200 cycle ALD processes at 200 0C
0.314 MJ
0.121 MJ
0.067 MJ
Inlet Pipeline Heating
Outlet Pipeline Heating
0.188 MJ
1.2 MJ
Energy input
0.203 MJ
0.077 MJ
0.279 MJ
System
control
Computer
0.210 MJ
0.210 MJ
0.75 MJ
Pre-treat
Wafer
Pulse
TMA
Pulse
H2O
A 20 nm Al2O3 Dielectric Gate on a 4” silicon wafer
Average energy consumption in ALD batch production:
0.7 MJ/wafer for 20 nm Al2O3 depositions
Scale-up
Case study: ALD of Al2O3
Analysis of energy flow in ALD process

## Slide 33
ALD process is energy intensive due to the process temperature requirement and
facility energy demand.
ALD process energy consumption is mainly decided by the process cycle time.
Energy (KJ/Cycle)
Cycle time (s)
Temperature (C)
ALD energy dependence on process parameters
Cycle time (s)
Energy (MJ)
ALD process energy reduction
(200 cycle operations)
18.2%
55.6%
ALD Process Energy Consumption
Case study: ALD of Al2O3

## Slide 34
Exergy balance and exergy efficiencies
Chart: 
| Heating | Material flow | Work
Inlet pipeline heating | 47.58
Outlet pipeline heating | 378.25
reactor heating | 902.75
input material | 13.6
列2 | 2256.75
Output material | 13.2
Exergy (KJ)
Exergy distributions for ALD of Al2O3 process (500 cycle operations)
Exergy associated with material flows is small compared to other distributions.
The exergy caused by work flow is the largest, which holds 63% of the total exergy input.
Case study: ALD of Al2O3

## Slide 35
Factors and levels
Design of ALD process for sustainability
Design objective is to minimize the gaseous emission and the nano-wastes and nano-particles
Factorial design table

## Slide 36
Experimental data
Design of ALD process for sustainability

## Slide 37
Gaseous emissions: ANOVA (Analysis of Variance)
The regression equation is Volume of CH4 per cycle (cm3) = 0.3683 - 0.002019 Purge Time (s) + 0.000066 Temperature (C).
Contour for minimization of gaseous emissions
Least emission (Dark green area) is found at longest purge time, and at moderate temperature.
Design of ALD process for sustainability

## Slide 38
Contour for minimization of gaseous emissions
Least emission of nano-particle (Dark green area) is found at shorter purge time, and at a comparable level of temperature.
Nano-particle emissions: ANOVA (Analysis of Variance)
The regression equation is No. of Nanoparticle per cycle = 239837500 - 7981250 Purge Time (s) + 285500 Temperature (C).
Design of ALD process for sustainability

## Slide 39
Summary
Deposition process is under a joint influence of precursor concentration and surface site saturation status.
Methane emissions are positively proportional to the film deposition process.
Temperature affects the ALD chemical process by changing the energy states of the surface species, and pulse time is directly related to the precursor dosage.
Size distribution, concentration, morphology and elements of nanoparticles are analyzed trough various instruments, including SMPS, UCPC, SEM, XRD.
Nano-particle emissions with diameter less than 100 nm are in the range of 6.0×105 and 2.5×106 particles in 25 cycles of Al2O3 ALD.
Energy consumption in ALD process is mainly determined by the cycle time and the process energy consumption could be significantly reduced by 64% when the cycle time is reduced from 18 s to 4 s.

## Slide 40
Thank you!
&
Questions?
Financial support from National Science Foundation under the grant of CMMI-1200940 is greatly acknowledged!